### Description

OS COLOR OPAQUE GLOSS WOOD STAIN is an elegant opaque semi-gloss wood finish for exterior and interior use. It is based on natural oils and is micro-porous, allowing the wood to breathe but protects against ingress of moisture.

It is longlasting, extremely weather- and UV-resistant, and will not crack, peel, flake or blister.

It has an exceptionally high solids’ content (85 %) which accounts for the long durability and large coverage. Covering in two coats, it allows the texture of the wood to be seen.

The ideal professional, low maintenance window finish (easy to renovate, just a further coat - no sanding or scraping).

Product based on natural oils

OS COLOR OPAQUE GLOSS WOOD STAIN is based on natural oils. Natural oils penetrate deeply into the wood, keeping it elastic and healthy, and preventing it from getting dry and brittle.

Shrinking and swelling are reduced. The wood is allowed to breathe. Moisture can evaporate.

Health and environment

OS COLOR OPAQUE GLOSS WOOD STAIN does not contain biocides nor preservatives  and can therefore also be used indoors. It is safe for man, animal and plant when dry and complies with German DIN 53 160  (fast to perspiration and saliva) and EURO Norm EN 71 (suitable for children’s toys). Test certificates available upon request.

The principle of OS COLOR to manufacture and supply only products which are safe and environmentally friendly during production as well as for appli
cation, resulted in the successful certification according to DIN EN ISO 9001 (quality management) and DIN EN ISO 14001 (environmental management) by the TÜV (Technical Control Board) Rhineland.

Uses

All exterior and interior woodwork.

Especially windows, clapboards (shutters), doors, but also fascias, fences, pergolas, trelliswork, trim, garden pavilions, dovecotes, beehives, flower boxes, green houses, garage doors etc.

Solid wood, plywood, laminated wood, new or weathered.

Excellent to re-new old wood finishes.

Can also be painted on stone and brick walls (not plaster), concrete and iron.

Colour Range

OS COLOR OPAQUE GLOSS WOOD STAIN is available in WHITE.

No. 2104 White

When using several cans with different batch numbers please mix together in one large container to ensure uniform coloration.

When used in dark indoor surroundings the high content of natural oils might cause yellowing.

No. of coats required

2 (requires 3 coats on dark surfaces)

Can sizes

0.375 litre, 0.75 litre,

2.5 litres (white only)

Larger volumes please enquire.

Coverage

approx. 10 sq.m per litre, on smooth wood approx. two coats, 17.5 sq.m per litre, one coat.

Rough or striated wood needs more material due to its surface structure.

Surface preparation

Wood surface must be clean, dry (maximum moisture content 20 %) and frost-free. Remove loose particles of old paint, wood fibres, dust, grease or mildew.

Glossy paints and varnishes: roughen surface with sand-paper.

TIP: to remove mildew, moss or lichen growth from old wood we recommend OS COLOR GARD CLEAN GREEN GROWTH REMOVER* (biologically decomposable).

If additional protection against blue stain, rot and mildew is desired (f. i. on pinewood), pre-treat with OS COLOR IMPREGNATION WR* Clear and allow 12 hours to dry. If biocidefree protection is preferred, treat with OS COLOR Wax Impregnation WOOD PROTECTOR (without synthetic biocides). If applied on Meranti, pre-treat with a primer.

Compatibility

Can be painted on:

OS COLOR WOOD WAX FINISHES,

OS COLOR COUNTRY COLOUR,

OS COLOR ONE COAT ONLY,

OS COLOR CLEAR OIL WOOD FINISH AND WOOD OILS

OS COLOR FENCE AND GARDEN STAINECOL,

OS COLOR WOOD STAIN AND PRESERVATIVE,

OS COLOR IMPREGNATION WR*,

OS COLOR WOOD PROTECTOR (biocidefree);

pressure-impregnated wood

and other micro-porous stains and paints in good condition.

Corrosion

In areas of high humidity the use of galvanised, non-oxidising nails and fasteners is recommended.

Method of application

By brushing.

OS COLOR OPAQUE GLOSS WOOD STAIN is ready to use. Do not thin. Stir well.

Use stiff quality OS COLOR BRUSH and apply thinly, evenly and thoroughly on clean, dry and frost-free surface.

Allow at least 12 hours drying time providing good ventilation. Then apply second coat.

New wood: where possible apply first coat on all sides of the wood before installation.

Windows must be thoroughly dry before closing, (drying time approx. 24 hours).

Cleaning of tools

With OS COLOR BRUSH CLEANER (benzole-free) or white spirit.

Drying time

approx. 12 hours - provide good ventilation (dust dry in approx. 6 hours).

Maintenance

Very simple. Just apply a further coat on clean, dry surface

Storage

Can be stored up to 5 years or more if  can is full and tightly closed. Store in dry place. If thickened by frost it will regain its consistency under normal temperatures within 24-36 hours.

Ingredients

85 % solids content

Base:        natural vegetable oils

(sunflower oil, soybean oil)

Pigments: iron oxide and organic

pigments, titanium dioxide

(white pigment),

all approved for use in the

food sector

Additives: water-repellent additives,

siccatives

Solvents: disaromatized white spirit -

(benzolefree - in compliance

with purity demands of the

European Pharmacopoeia)

Full declaration of ingredients upon request

Technical Data

Specific gravity: 1.2 - 1.4 g/cm3

Viscosity:          48-58”, 4 mm according

to DIN 53 211, creamy

Odour:              faint/mild, odourless

after drying

Flashpoint:    Flammable-Flashpoint

Setaflash ASTM D > 55 °C.

Dried surface hardly flammable according to TL A-053.

Fire conduct in compliance with demands of German DIN 4102 (fire conduct of building materials and components) Class B 2 (normal inflammability).

Caution

Keep out of reach of children. Do not fill into containers normally used for food and drink. Work in areas with good ventilation. Do not apply in the presence of naked flames, hot surfaces or unprotected electrical equipment. In case of contact with eyes rinse immediately with plenty of water.

Wash out any cloths that have been used to clean brushes immediately or store in a airtight container (danger of combustion).

* Use biocides safety. Always read the label and product information before use.