| Tortread™ SP floor paint | AK724 |
| --- | --- |

| intended uses |  | A single-pack general purpose, light duty floor coating for use in warehouses, factories, work shops, garages, showrooms etc. |
| --- | --- | --- |

| product description |  | A tough urethane alkyd blended with long oil alkyd pigmented with pigments and thinned with low aromatic white spirit. |
| --- | --- | --- |

| product information |  | Product reference | AK724 |
| --- | --- | --- | --- |
|  |  | Volume solids | 47+/-2% |
|  |  | Typical thickness | 47+/-2 microns dft per coat |
|  |  | Theoretical coverage | 10 square metres per litre per coat |
|  |  | Practical coverage | Reduce theoretical coverage by approximately 20% |
|  |  | Appearance/Colour range | Semi Gloss / Black, Red, Mid Grey, Green, 08E51, 00A05, 18E53 and supplementary colours. See colour card. |
|  |  | VOC content | EU limit value for this product (cat A/i): 500 g/l . This product contains max 500 g/l VOC |

| application details |  | Mix ratio | N/A |
| --- | --- | --- | --- |
|  |  | Method of application | Preferred short pile roller but can be airless sprayed (0.015” tip and 2000 psi atomising pressure). 2 coats normally required. |
|  |  | Thinner | Tor TH10 (when required) |
|  |  | Cleaner | Tor TH10 for cleaning equipment |
|  |  | Pot Life | N/A |
|  |  | Drying time |  |
|  |  | Substrate Temperature | Touch Dry | Hard Dry | Overcoating Interval |
|  |  |  |  |  | Minimum* | Maximum |
|  |  | 20oC | 4 hours | Within 16 hours | 8 hours | 7 days |
|  |  | Note: Drying/curing times will be shortened by higher temperatures and lengthened by lower temperatures. *Inadequate ventilation will affect drying/curing performance. |

| storage and handling |  | Storage | Store in a safe place out of the reach of children |
| --- | --- | --- | --- |
|  |  | Pack Size | 5 litres |
|  |  | Flash point | 42oC |
|  |  | Product weight | 1.20+/-0.03 kilos/litre |
|  |  | Shelf life | 2 years in unopened containers |

| surface preparation |  | Ensure all surfaces are clean, sound, dry and free from oil grease, grime and other surface contaminants. Bare Concrete: Ensure dry (less than 5.5 on protimeter screed scale). Surfaces should be cleaned by best available method to remove laitance, oils, etc. and to “open up” substrate (eg. vacu-blast, disc grind, scabble, acid etch etc, hot compressed air treatment for deep oil removal). Apply Tor Stabilising Sealer (AK602) to prepared surfaces. Previously Painted: Perform adhesion check. If suspect – remove existing paint. If sound – wash, degrease and abrade. Apply Tor Stabilising Sealer (AK602) to bare areas only. |
| --- | --- | --- |

| limitations |  | Will only withstand pedestrian and light rubber wheeled vehicular traffic. Not suitable for heavy duty use or in high humidity areas such as shower rooms, swimming pools etc. |
| --- | --- | --- |

| safety precautions |  | A copy of the appropriate Health & Safety Data Sheet should be consulted prior to using the product. This can be faxed if urgently required. Minimum precautions for all paints: Avoid skin and eye contact i.e. wear gloves, goggles, etc Ensure good ventilation, mechanical if necessary. Store and use away from heat and flame. Do not eat or smoke in the vicinity of work. Wash hands before eating. Refer to supply container for additional warning labels. |
| --- | --- | --- |

| definitions |  | Tolerances | All information quoted in this data sheet is subject to normal manufacturing tolerances. |
| --- | --- | --- | --- |
|  |  | Practical coverage | Practical coverage can vary considerably depending on method of application, surface roughness, weather conditions and complexity of the structure. |
|  |  | Pot Life | Applies only to two component products and refers to the time the mixture remains usable. |

| disclaimer |  | The information contained herein is to the best of our knowledge true and accurate and is given in good faith but without warranty. The user will be deemed to have satisfied him/herself independently as to the suitability of our products for his/her own particular purpose. In no event shall Tor Coatings be liable for consequential or incidental damages. This document will normally be updated at least every two years. It is the users responsibility to ensure that they have the current copy. |
| --- | --- | --- |

### Updated: Feb 2011

AK724