PRODUCT:-  ACRYLIC COATING (for roofs)

REFERENCE:-  W/488/1001

COLOUR:- RED, GREY, GREEN

FINISH:-  SEMI-GLOSS

TYPE:-  AQUEOUS MIXED COPOLYMER

DISPERSION

TYPICAL SG:-  1.16 AT 20(C

TYPICAL VISCOSITY:-  3.0P AT 25(C

TYPICAL TOTAL SOLIDS:-  44.9% BY WEIGHT

FLASH POINT:- NOT APPLICABLE

RECOMMENDED THINNERS:-  WATER

APPLICATION:-  BY BRUSH OR ROLLER

(DO NOT APPLY WHEN THE

TEMPERATURE IS BELOW 5(C)

*COVERAGE GUIDE:-  7-12 SQ. METRES/LITRE

*DRYING TIME:-  SURFACE DRY -    2  HOURS

THROUGH DRY -  12 HOURS

(COLD,DAMP CONDITIONS WILL PROLONG THESE TIMES)

USES:-  AS A PROTECTIVE AND

DECORATIVE FINISH TO

ASBESTOS SHEETS, MASONRY,

RENDERING AND PLASTER

WORK

STORAGE:-  PROTECT FROM FROST AND

ABNORMAL HEAT

HEALTH & SAFETY:-  SEE SHEET HSD 'B’

*BY BRUSH TO A DRIED FILM THICKNESS OF 20-25 MICRONS AT 20oC.