PRODUCT:-  ANTICORROSIVE RED OXIDE

REFERENCE:-  G150/65

COLOUR:-  RED

FINISH:-  GLOSS

TYPE:-  MODIFIED ALKYD

TYPICAL SG:-  1.16 @ 20(C

TYPICAL VISCOSITY:-  3.5 POISE @ 25(C

TYPICAL TOTAL SOLIDS:-  66% BY WEIGHT

49% BY VOLUME

FLASH POINT:-  ABOVE 32(C

RECOMMENDED THINNERS:-  WHITE SPIRIT OR TURPS SUBS

APPLICATION:-  BY BRUSH

*COVERAGE GUIDE:-  11 SQ. METRES PER LITRE

*DRYING TIME:-  SURFACE DRY  5  HOURS

HARD DRY       24 HOURS

USES:-A GENERAL PURPOSE,

VERSATILE PAINT, GIVING

ECONOMICAL PROTECTION AND

MAINTENANCE OF STRUCTURAL

STEEL, WHEN APPLIED TO

PROPERLY PREPARED SURFACES.

DRIES WITH A DURABLE GLOSS

FINISH.

VOC:-   394 g/litre

HEALTH & SAFETY:-  SEE SHEET HSD A1L

*BY BRUSH TO A DRIED FILM THICKNESS OF 40 - 50 MICRONS AT 20oC.

Issued October 2004